# Text boxes

FeO

0.2mm

0.2mm

Mi

Q

Q

##### PLATE 1:  #25  432.0m  Clifton Formation

FIGURE 1   Plane polarised light

FIGURE 2   Crossed polarisers

Biomicrite limestone in which calcareous shell fragments (F) and detrital quartz grains (Q) are supported by iron-oxide/hydroxide (FeO)-stained micrite matrix (Mi) in which fine dolomite rhombs (Do) have precipitated.

0.2mm

Q

F

F

Do

Mi

Do

FeO

FeO

FeO

Q