# Text boxes

C2

0.2mm

0.2mm

P

Q

Q

##### PLATE 4:  #15  566.9m  Pember Mudstone  (cont.)

FIGURE 1   Plane polarised light

FIGURE 2   Crossed polarisers

Macroporosity (P) is confined to localised, relatively clean areas, but even here intergranular spaces are partly filled by authigenic kaolinite (K) and thinly dispersed detrital clay (C1).  Elsewhere, intergranular spaces are completely filled by detrital clay matrix (C2).  Framework grains are mainly quartz (Q) and K-feldspar (KF) (stained brown).

0.2mm

C1

Q

KF

K

C2

K

C1

Q

P

KF